[image: image1.jpg]Working Pressure 16
Test Body 24 Bar
Pressurd seat 175
Working Temp. £65°C
Media Available Water
shackles Carkon steel
0—Ring NER
gaskeT NER
contact Ductie Tron
cover Ductile Iron
Disc Ductlle Iron
0-Ring NER
U—Ring NER
0—Ring NER
Bonnhet Ductie Iron
tem Nut Ductle Iron
fTem 2cri3
Bod Ductle Iron
Name Material

DN130





[image: image2.jpg]Working Pressure 16
Test Body 24 Bar
Pressurd seat 175
Working Temp. LESE
Media Available Water
shackles arbon steel
0-Ring NER
gaSKeT NER
contact Ductlle Iron
cover Ductile Iran
Disc Ductile Iron
0-Ring NER
0-Ring NER
0-Ring NER
Bonnet Ductile Iran
Tem Nut Ductlle Iron
fem 2Cr13
Bod Ductile Iron
Name Material

DN100
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DN D c |ag t | n-ed | f
gosket NER NBR
Seat Tuctlle Tron | AS26-65-45-12
Disc [A536-65-45-12+EPDM
Stem Staneless steel|  SS410
0 Ring NER NBR
0 Ring NER NBR
0 Ring NER NBR
0 Ring NER NBR
Cap Ductile Iron | AS36-65-45-12
Connector Tuctile Iron | AS36-65-45-12,
Stem Nut Tuctlle Iran A536-65-45-12
Gland Nut Ductile Iron | AS36-65-45-12
Bolt Stainless steel A3
0 Ring NER NBR
0 Ring NER NBR
Choln uctile Iran | AS36-65-45-12
Body part A Ductlle Iron | AS36-65-45-12
0 Ring NER NER
Flange Ductile Tran | AS36-65-45-12
Bolt A3 A3
Vista Ductile Iron | AS36-65-45-12
Body part B Tuctlle Iran | AS36-65-43-12
Ports Material
Fire Hydrant
DN100-150





